## Slide 1
Spin dynamic under resonant excitation
|3,+2>
E
0
+1
+2
+3
Mz
s-
s+
tff
Gin
Gout
= Dark time dependence of the amplitude of the pumping transient (ΔI/I, inset) gives an estimation of 75 ns for the h-Mn relaxation time.

## Slide 2
Coherent dynamics under magnetic field
B┴
B//
B=0
Magnetic field parallel to growth axis (B// ): tune splitting of levels and block the strain induced dynamics
In plane magnetic field (B┴ ): induces a coherent precession
Polar. rate
Bz=0.2T
Bz=0.09T
Bz=0.05T
B=0T
Bx=0.13T
Bx=0.23T
Bz=0.2T
B=0T
Bx=0.23T
Bx=0.42T
Bz=0.2T
B=0T
Bx=0.23T
Bx=0.42T

## Slide 3
B┴
B//
B=0
B//
B┴
Coherent dynamics under magnetic field
= e-Mn energy levels
= Model: coherent dynamics controlled by local strain
A. Lafuente-Sampietro et al., Phys. Rev. B 92, 081305(R) (2015)

## Slide 4
Magneto-optical properties: model
A. Lafuente-Sampietro et al., Phys. Rev. B 93, 161301 (R) (2016)
= Modeling with a spin effective Hamiltonian including:
Zeeman energy (e, h, Cr)
Carrier-Cr exchange
e-h exchange interaction and hh-lh mixing in a low symmetry QD.
Effective spin temperature
Magnetic anisotropy D0
s-
(1)
(2)
(3)
(4)
s+
(5)
(6)
s+
Bz
Sz=0
Sz=+1
Sz=-1
ISz=-1,+1>
ISz=+1,-1>
ISz=0,+1>
ISz=+1,+1>
ISz=-1,-1>
ISz=0,-1>
ISz=-1,+2>
ISz=+1,-2>
ISz=+1,+2>
ISz=0,+2>
s-
(1)
(2,3)
(4)
(5)
0
E
D0
X-Cr
Cr
(6)
D0

## Slide 5
QD3
QD3
X2-Cr
X-Cr
s+
s+
s-
s-
X2-Cr
X-Cr
Cr
= With two excitons in the QD, the exchange interaction with the Cr spin vanishes: mirror symmetry in the optical transitions.
Magneto-optical properties of Cr-doped QDs
s-
I-1>
I+1>
Sz=+1
s+
Sz=0
Sz=-1
px
py

## Slide 6
A material issue: Hole-Cr exchange interaction in CdTe QDs
s-
s+
Sz=-1
Sz=-1
s-
s+
Sz=0
Sz=-1
Sz=+1
E
Bz
Sz=-1
Sz=-1
- The e-Cr exchange interaction is weak and ferromagnetic.
- Polarization under magnetic shows that h-Cr exchange is antiferromagnetic.
- A material issue: h-Cr is found to be ferromagnetic in all the bulk II-VI compounds?
- But Cr is a tricky system where the 3d orbitals are close to the top of the valence band… influence of
strain on the Cr2+ to Cr3+
transition?
Sz=+1
Sz=0
Sz=+1
Sz=0
s-
s+

## Slide 7
Magneto-optical properties: model
= The thermalization (below 50K) explains why the ±2 Cr spin states are not observed. The thermalization under B is qualitatively reproduced.
= Not possible to probe the spin states ±2 at higher temperature with these QDs.
D0=2,2 meV
Teff=20K

## Slide 8
= Two different relaxations times linked to two different relaxation processes
Dynamics of Cr under optical excitation
Resonant pumping transient after:
A non-resonant excitation
A resonant excitation
tCr,2 ≈ 2 ns
tCr,1 ≈ 20 ns

## Slide 9
Dynamics of Cr under optical excitation
Heating with a non-resonant probe in-between pump pulses
E
Sz=-1
Sz=0
D0
0
Sz=+1
= The probe pulse create a non-equilibrium state, populating the states Sz = ±1
E
Sz=-1
Sz=0
D0
0
Sz=+1
= During the dark time, the non-equilibrium state relaxes, repopulating Sz = 0
tCr,1
= Sz = ±1 can relax toward Sz = 0 via a 1 phonon mechanism with a characteristic time tCr,1
= The pumping transient after a heating pulse probe the transfer from Sz = ±1 to Sz = 0

## Slide 10
Dynamics of Cr under optical excitation
Relaxation in the dark with only a pumping pulse
E
Sz=-1
Sz=0
D0
0
Sz=+1
= During the drak time, the state Sz = -1 is repopulated from Sz = 0 and Sz = +1
E
Sz=-1
Sz=0
D0
0
Sz=+1
= The pump pulse empty the states Sz = -1, transfering the population to Sz = +1 and Sz = 0
tCr,1
= Sz = +1 can transfer to Sz = +1 via a 2 phonon mechanism involving an excited state with a characteristic time tCr,2
= Sz = ±1 can relax toward Sz = 0 via a 1 phonon mechanism with a characteristic time tCr,1, longer than tCr,2
= The pumping transient after a heating pulse probe the transfer from Sz = ±1 to Sz = 0
tCr,2
Excited state